

Chemical Resistance

Estrabond **ECO V10**

**20c & 100°c / 68F & 140F**

|  |  |  |  |
| --- | --- | --- | --- |
| Medium Type | Concentration**%** | Test duration 6 months**20c / 68F** | Test duration 30 days**60c / 140F** |
| Acetic acid | 10 | R | LR |
| Acetone b.p. 56c / 133F | 100 | R | R |
| Ammonia solution | conc | R | R |
| Aniline | 100 | SR | - |
| Anti Freeze |  | R | SR |
| Apple juice |  | R | R |
| Asphalt |  | R | R |
| Barium salts |  | R | R |
| Battery acid |  | LR | NR |
| Beer alcoholic  |  | R |  |
| Benzene | 100 | R | LR |
| Brake fluid |  | R | R |
| Butane gaseous | 100 | R | R |
| Butane liquid | 100 | R |  |
| Caustic potasch | 50 | R | R |
| Caustic soda | 50 | R | R |
| Chlorine, liquid | 100 | NR | NR |
| Citric acid aqueous | Cold saturated | R | LR |
| Cyclohexanone | 100 | R | LR |
| Detergent solution |  | R | R |
| Dibutyl phthalate |  | R | R |
| Diethyl ether | 100 | SR |  |
| Dishwashing detergents |  | R | R |
| Ethyl alcohol, not denatured | 100 | R | SR |
| Formic acid | 10 | R | R |
| Fuel oils paraffin | 100 | R | R |
| Glycerin | 100 | R | R |
| Glycol | 100 | R | R |
| Hydrochloric acid | 10 | NR | NR |
| Hydrofluoric acid | 40 | LR | LR |
| Hydrogen peroxide | 30 | R |  |
| Lactic acid aqueous  | 10 | SR | LR |
| Linseed oil |  | R | R |
| Methanol | 100 | R | SR |
| Methyl ethyl ketone | 100 | R | LR |
| Nitric acid | 10 | NR | NR |
| Ozone 0.6 ppm |  | LR |  |
| Petrol benzene |  | R | R |
| Propane gas | 100 | R | R |
| Pyridine | 100 | R |  |
| Saline water |  | R | R |
| Silicon oils |  | R | R |
| Sodium hypochlorite acq | SR5 | R | LR |
| Sodium chloride – salt |  | R | R |
| Sulphur | 100 | R | R |
| Sulphuric acid | 10 | R | LR |
| Toluene | 100 | R | LR |
| Trichlorethylene | 100 | LR | LR |
| Xylene | 100 | R | LR |

**Keys:-**

R = resistance

SR = some resistance

LR = limited resistance

NR = No resistance

**Disclaimer**

The information contained herein is to our knowledge accurate and reliable as of the date of publication. Intechem extends no warranties and makes no representations as to the accuracy or completeness of the information contained herein, and assumes no responsibility regarding the consequences of its use or for any printing errors.

Our products are intended for sale to industrial and commercial customers. It is the customer's responsibility to inspect and test our products in order to satisfy himself as to the suitability of the products for the customer's particular purpose. The customer is also responsible for the appropriate, safe and legal use, processing and handling of our products. Nothing herein shall constitute any warranty (express or implied, of merchantability, fitness for a particular purpose, compliance with performance indicators, conformity to samples or models, non-infringement or otherwise), nor is protection from any law or patent to be inferred. No statement herein shall be construed as an endorsement of any product or process.

Insofar as products supplied by Intechem is used in conjunction with third party materials, it is the responsibility of the customer to obtain all necessary information relating to the third party materials and ensure that Intechem’s products when used together with these materials are suitable for the customer’s particular purpose. No liability can be accepted in respect of the use of Intechem’s products in conjunction with other materials. The information contained herein relates exclusively to our products when not used in conjunction with any third party materials.

All rights reserved. Copyright **(C)** 1996, Estrabond is a registered trade mark **# 2454305**

Intechem Polymer Systems & Co.

205 Parkway House, sheen Lane, London SW14 8LS, United Kingdom**.**

Tel: + 44, 20, 8878 6578 email: Estrabond@btconnect.com